Natural Radioactivity in the RCC Building materials used in the Southern districts of Manipur, India

ABSTRACT:

This study aimed to measure the amount of natural radiation found in different building materials used in the southern parts of Manipur, India. These materials include cement, concrete, sand, and bricks, which are commonly used in Reinforced Cement Concrete (RCC) construction.

The study looked at the levels of three naturally occurring radioactive elements: Radium-226 (226Ra), Thorium-232 (232Th), and Potassium-40 (40K).

Observations:

- Portland cement had average radioactivity levels of 40 BqKg-1 for 226Ra, 38 BqKg-1 for 232Th, and 1644 BqKg-1 for 40K.

- Concrete had 34 BqKg-1 for 226Ra, 61 BqKg-1 for 232Th, and 547 BqKg-1 for 40K.

- Sand had 46 BqKg-1 for 226Ra, 112 BqKg-1 for 232Th, and 1580 BqKg-1 for 40K.

- Bricks had 31 BqKg-1 for 226Ra, 148 BqKg-1 for 232Th, and 1388 BqKg-1 for 40K.

The study also discussed how this radiation might affect people. The average annual radiation dose people might receive from these materials is about 1.7 millisieverts per year (mSvy-1), which may vary between 0.8 and 3.0 mSvy-1.

The gamma radiation index, which helps to estimate the safety of the materials, was on average 1.0 (ranging from 0.5 to 1.9). A value higher than 1 could suggest higher radiation exposure.

Finally, the extra yearly radiation caused specifically by these building materials ranged from 0.1 to 2.3 mSvy-1, with an average of 1.0 mSvy-1.

Key words:

Natural radioactivity, Gamma spectrometer, RCC Building materials, Annual effective dose, Excess dose

- INTRODUCTION

Most often, assessing the risk that environmental radiation exposure poses to humans, attention has been focused on the distribution and concentration levels of naturally occurring radionuclides in our surroundings [1]. This is because natural radiation accounts for the major contribution of external radiation dose to the world population [2]. The chance of being exposed to radiation from natural radionuclide contamination in construction materials, both internally and externally, is very high [3-4]. It is observed that building materials used for constructing houses, such as concrete, brick, sand, marble, granite, portland cement, gypsum, etc., are mainly contaminated with natural radionuclides such as Uranium (238U) and Thorium (232Th), their decay radionuclide series, and radioactive Potassium (40K) [5]. The largest radiation exposure for the general population as well as occupational workers comes from radon, thoron, and their decaying radioisotopes [6]. These two noble gases are present in the ambient air and in the indoor atmosphere [7]. These gases are expected to be more concentrated indoors than outdoors. Radon and thoron radioactive gases found in nature are considered the primary risk factor of lung cancer for non-smokers and the second most common cause of this cancer in smokers [8]. Li et al [9] have reported that the risk of lung cancer is significantly associated with residential radon exposure. The high levels of 226Ra and 232Th in the environment are mainly linked to radon and thoron exhalation. The natural radioactivity contaminants in a building material or soil samples are usually assessed from 226Ra, 232Th and 40K content. The indoor average annual effective dose of the world-wide due to natural gamma radiation from building materials is estimated to be about 0.4 mSvy-1 [10]. Research conducted on construction materials including granite and phosphogypsum revealed an enhancement of indoor absorbed dose rate up to five times greater than the dose criterion [11], whereas building materials collected from Yan’an, China, may be utilized safely as construction materials [12].

The study area includes Kackching, Thoubal and Churchandpur districts of Manipur, India. This Kakching district has an area of 190 square-kilometre (sqkm) and a total population of 135,481, Thoubal district has an area of 324 sqkm with a total population of 286,687 and Churchandpur is having an area of 4,750 sqkm with a total population of 274,143 [13]. In this study area, there has been a rapid replacement of the old traditional houses (mainly assam type houses) with Reinforced Cement Concrete (RCC) structures for livelihood, during the last few decades. Studies on indoor natural gamma radiation from radioactive contamination in the construction materials of various types of houses, it has been reported that RCC buildings exhibit higher annual effective doses than other houses in this area [14-16]. Most people spend their maximum time in indoor (about 80%), hence, the concentration of radionuclides in building materials is crucial for determining population exposure. Thus, it is important to monitor and regulate the radioactivity levels in building materials to ensure the safety of residents and workers in the area. By conducting regular assessments, authorities can make informed decisions to mitigate any potential health hazards associated with exposure to radioactive contaminants.

- MATERIALS AND METHODS

Radiological Analysis of Building Materials

  - Sample collection and preparation

Within the study area, a total of fifteen (15) samples of building materials were collected, crushed into small pieces, and dried in a hot air oven for twenty-four hours at around 100° Celsius. It is then crushed into a fine powder, homogenized, and sieved through a 0.45 mm mesh size. Approximately 250 g of this homogeneous fine mesh of each sample is packed inside a cylindrical plastic container that has a predetermined shape (3" in diameter by 5" in height), is weighted, and is appropriately sealed to prevent radon or thoron gas from escaping [17]. The treated samples are kept in a safe place for approximately four weeks to bring 226Ra and 232Th, as well as their corresponding daughter nuclides, to equilibrium [14].

  - Gamma spectrometry

Using Gamma spectrometer having HPGe detector, with a relative efficiency of 35% and a resolution of 1.8 keV for the gamma emission of the 1.33 MeV of 60Co, the specific activity concentration of 226Ra, 232Th, and 40K in the samples was determined. A mixed point source of 241Am (59.5 keV), 137Cs (661.7 keV), and 60Co (1173.2, 1332.5 keV) was employed for the energy calibration of the HPGe detection system. Once it had reached equilibrium with its daughter radio-isotopes, the uranium-ore standard (IAEA-RGU-1, uranium ore) with an activity of 4940 Bq/kg was utilized for efficiency calibration. Table 1, is the list of the daughter radionuclides and their energies that were used to calibrate efficiency.

A fourth-order polynomial was fitted to the energy versus efficiency plot, and this polynomial was then utilized to assess the radionuclides of interest or their efficiencies. The activity of 40K was determined from 1460 keV photo peak; the activity of 226Ra was assessed from a gamma lines of 214Bi at 1766 keV and 352 keV of 214Pb; and the activity of 232Th was determined from the most prominent gamma lines of 208Tl at 510.6, 583.2, and 2610 keV, 212Bi at 727.2 KeV, and 212Pb at 238.6 KeV [18-24].

  - Radioactivity evaluation

The activities of 226Ra, 232Th series, and 40K are evaluated using the following equation [25]:

A(Bqkg-1)=NεβM                                                                          (1)

Where, N = the net gamma counting rate (counts per second) in channel E, ε = the detector efficiency of the specific gamma-ray with energy E, β = the absolute probability of gamma transition at energy E and M = the mass of the sample (kg).

  - Gamma index ‘I’or Activity concentration index

Gamma index ‘I’ or Activity concentration index is defined to investigate the applicability of building materials in construction. It is given by the following expression [26] as;

I = ARa /300 + ATh /200 + AK /3000 ≤ 1				        (2)

where ARa, ATh and AK are the activity concentration of 226Ra, 232Th and 40K in Bqkg-1, respectively.

This is a straightforward reference criterion for figuring out whether building materials are applicable. When this value is more than unity, there may not be a considerable exposure that could have a negative impact on one's health [27].

  - Absorbed Dose Rate (D)

The absorbed Dose Rate (D) resulting from naturally occurring gamma radiation in air was computed using the guidelines provided in EC Report 112 for a standard room dimension and common building materials containing naturally occurring radionuclides 226Ra, 232Th, and 40K [26] as;

D (nGyh-1) = 0.92 ARa +1.1 ATh + 0.08 AK					(3)

  - annual effective dose (Deff)

The annual effective dose (Deff) is calculated by using the dose conversion ratio of 1.0 SvGy-1 from the absorbed dose in air received by an adult as well as a value of 0.8 as an indoor occupancy factor [10]. Deff (mSvy-1) due to gamma radiation from building materials is determined as;

Deff (mSvy-1) = D (nGyh-1) X 8760(h/y) X 0.8 X 1.0 (SvGy-1) X 10-6		(4)

- RESULTS AND DISCUSSION:

The districts of Kakching, Thoubal and Churchandpur are in southern part of Manipur, India, constitute the study area. The main materials used for this RCC building houses are portland cement, concrete, sand, and bricks, respectively. Using a gamma spectrometer with HPGe detector, the natural radioactivity contaminant levels of such building materials in study area are determined. The measured radioactivity contaminant levels of 226Ra, 232Th and 40K of these RCC building materials are shown in Table 2. All portland cements and 2 types of sand (Table 2: sand 3 & sand 4) were imported from neighbouring states. The average specific activity of 226Ra was 39 Bqkg-1 (range: 22 to 60 Bqkg-1), which is slightly higher than the world average value of 35 Bqkg-1 [10].  Whereas the average specific activity 232Th was 90 Bqkg-1 (range: 23 to 198 Bqkg-1) and 40K was 1313 Bqkg-1 (range: 431 to 2008 Bqkg-1) which were moderately higher than the corresponding global average values of 30 Bqkg-1 and 400 Bqkg-1, respectively [10].

The calculated values of adsorbed dose rate (D), annual effective dose (Deff), gamma index (I) and excess dose due to building materials (Dex) are shown in Table 2. The absorbed dose rate due to naturally occurring gamma radiations in air for a standard room dimension and for common building materials due to natural radionuclides 226Ra, 232Th and 40K ranged from 117 nGyh-1 (concrete 1) to 431 nGyh-1 (sand 4) with an average value of 243 nGyh-1, which was observed to be higher than the world average (populated weighted) indoor absorbed gamma dose rate of 84 nGyh-1 [10].  Absorbed dose rate for different types of building materials from this study area is shown in Figure 1. The percentage contribution to the absorbed dose rate from the radioactive contaminants of 226Ra, 232Th and 40K from different building materials used, along with their mean, is shown in Figure 2.

The average annual effective doses calculated from building materials were found to be 1.0 mSvy-1 from concrete, 1.5 mSv-1 from portland cement, 2.0 mSvy-1 from sand, 2.1 mSvy-1 from brick, and 0.6 mSv-1 from soil. Deff of the samples of building material ranged from 0.8 mSvy-1 (concrete 1) to 3.0 mSvy-1 (sand 4) with an average value of 1.7 mSvy-1, which is observed to be higher than the world average value of 0.5 mSvy-1 [28] and 0.4mSvy-1 [10].

The gamma index, which assesses excess gamma radiation from construction materials, showed an average value of 1.0 [range: 0.5 (concrete 1) to 1.8 (sand 4)], which is same as the suggested value of unity [26]. The occupant's annual excess effective dose (Dex) was evaluated from building materials by subtracting the annual effective dose from the undisturbed earth's crust [26]. Figure 3 is the graph between annual effective dose (mSvy-1) and Gamma index” I”, showing annual effective dose and excess dose “Dex” to the residents due to the building materials in this study area.

Radioactivity analyses of the building materials used show values that are comparatively higher than those in the world and the country [Table 3]. I, D and Deff of this study were observed to have higher values than other national studies except the study in Valley region, Manipur, by Sharma et al [44], Una, Himachal Pradesh, by Bala et al [40], which is comparable. Other comparable studies outside the country were also observed in Pakistan by Rahman et al. [30], Ankara, Turkey by Turhan et al. [32] and in Iran by Abbasi [35]. However, the maximum of ranges given for I, D, and Deff in global studies; radioactivity contaminant of European building material by Trevisi et al. [29] is showing exceptionally higher values compared with other studies.

- CONCLUSIONS

A study was carried out in the southern districts of Manipur, India, to find out how much natural radiation is present in materials commonly used to build homes and buildings, such as cement, concrete, sand, and bricks.

The measured levels of naturally occurring radioactive elements 226Ra, 232Th, and 40K in these materials, especially sand and bricks, were higher than global averages. The overall radiation dose people might receive from these materials was also found to be above the world average.

For example, bricks and sand showed the highest levels of radiation, followed by cement and concrete. The study also found that the radiation absorbed by people living in such buildings could range from 0.1 to 2.3 mSvy-1, with an average of 1.0 mSvy-1, which matches the safety guideline but still calls for attention.

With the construction of homes to provide comfort and protection, it is equally important to ensure they are safe and healthy environments. Understanding the materials used is the first step toward making informed choices—choices that reduce hidden risks like radiation exposures. By selecting safer building materials and monitoring their quality, it is viatl to protect not only the present well-beings but also that of future generations. A truly safe home is not just defined by its structure, but by the thoughtfulness and care put into every material used in its construction.

Table 1: Radionuclide daughter products and their energies used for efficiency calibration

| Radionuclides | Energy (Kev) |
| --- | --- |
| 232Th | 63.34 |
|  | 92.79 |
| 226Ra | 186.22 |
| 214Pb | 352.36 |
| 214Bi | 609 |
|  | 935.21 |
|  | 1121 |
|  | 1766.8 |

Table 2: Radiological parameters of building materials used in the valley region of Manipur.

| Sample Type | Radionuclide Concentration (Bqkg-1) |  |  | Gamma I | D nGyh-1 | Deff mSvy-1 | Dex mSvy-1 |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 226Ra | 232Th | 40K |  |  |  |  |
|  | Four portland cement Samples |  |  |  |  |  |  |
| Portland Cement 1 | 33±4 | 64±5 | 1214±71 | 0.8 | 198 | 1.4 | 0.7 |
| Portland Cement 2 | 58±4 | 35±2 | 1634±151 | 0.9 | 223 | 1.6 | 0.9 |
| Portland Cement 3 | 31±3 | 29±6 | 1824±137 | 0.9 | 206 | 1.4 | 0.7 |
| Portland Cement 4 | 38±5 | 23±4 | 1904±121 | 0.9 | 213 | 1.5 | 0.8 |
| Average value | 40±12 | 38±18 | 1644±308 | 0.9 | 210 | 1.5 | 0.8 |
|  | Three concrete Samples |  |  |  |  |  |  |
| Concrete 1 | 24±3 | 41±5 | 627±91 | 0.5 | 117 | 0.8 | 0.1 |
| Concrete 2 | 41±7 | 77±4 | 583±141 | 0.7 | 169 | 1.2 | 0.5 |
| Concrete 3 | 36±6 | 66±3 | 431±162 | 0.6 | 140 | 1.0 | 0.3 |
| Average value | 34±9 | 61±18 | 547±103 | 0.6 | 142 | 1.0 | 0.3 |
|  | Four sand Samples |  |  |  |  |  |  |
| Sand 1 | 31±2 | 59±7 | 1328±102 | 0.8 | 200 | 1.4 | 0.7 |
| Sand 2 | 40±5 | 73±5 | 1213±56 | 0.9 | 214 | 1.5 | 0.8 |
| Sand 3 | 51±7 | 118±11 | 1803±176 | 1.4 | 321 | 2.2 | 1.5 |
| Sand 4 | 60±5 | 198±18 | 1976±154 | 1.8 | 431 | 3.0 | 2.3 |
| Average value | 46±13 | 112±63 | 1580±367 | 1.2 | 291 | 2.0 | 1.3 |
|  | Four brick Samples |  |  |  |  |  |  |
| Brick 1 | 29±5 | 176±8 | 1123±57 | 1.4 | 310 | 2.2 | 1.5 |
| Brick 2 | 32±3 | 68±9 | 1441±123 | 0.9 | 220 | 1.5 | 0.8 |
| Brick 3 | 41±8 | 156±9 | 2008±201 | 1.6 | 370 | 2.6 | 1.9 |
| Brick 4 | 22±4 | 193±8 | 980±73 | 1.4 | 311 | 2.2 | 1.5 |
| Average value | 31±8 | 148±56 | 1388±456 | 1.3 | 303 | 2.1 | 1.4 |
|  | Soil Samples analysis of the study area |  |  |  |  |  |  |
| Average value* | 52 | 106 | 1110 | --- | --- | 0.7 | --- |

*Average value of the reported data in [22-24]

Figure 1: Absorbed dose rate for various types of building materials

Figure 2: Percentage contribution from 226Ra (Ra-226), 232Th (Th-232) and 40K (K-40) contaminant to the Absorbed Dose rates for different types of building materials

Figure 3: Graph between Annual effective dose (mSvy-1) and Gamma index” I”, showing effective dose and excess dose “Dex” due to building materials of the study area.

Table 3: Radiological parameters of building materials as reported in various studies.

| Studies | Activity concentration (Bqkg-1) |  |  | I range | D (nGyh-1) range | Deff (mSvy-1) range |
| --- | --- | --- | --- | --- | --- | --- |
|  | 226Ra | 232Th | 40K |  |  |  |
| European Trevisi et al [29] | 53 2-2620 | 41 1-463 | 425 1-3120 | 0.5 0.0-12.1 | 67 2-1620 | 0.4 0-9.9 |
| Pakistan Rahman et al [30] | 2-799 | 1-124 | 7-1272 | 0.0-3.7 | 2-497 | 0-3.0 |
| Jordanian AI-Jundi et al [31] | 28-70 | 6-33 | 31-59 | 0.1-0.4 | 18-55 | 0.1-0.3 |
| Ankara,Turkey Turhan et al [32] | 1-145 | 1-170 | 2-1792 | 0-1.9 | 1-244 | 0-1.5 |
| Kutahya, Turkey Cetinkaya etal [33] | <2-81 | <1-25 | <8-819 | 0-0.7 | <2-87 | 0-0.5 |
| NW-Nigeria Garba et al [34] | 47-63 | 24-32 | 219-257 | 0.3-0.5 | 48-58 | 0.8-0.9 |
| Qassim, KSA, EL-Taher, [18] | 13-38 | 13-49 | 64-340 | 0.1-0.5 | 18-54 | 0.1-0.4 |
| Iran, Abbasi [35] | 4-94 | 7-172 | 557-1539 | 0.2-1.7 | 29-212 | 0.2-1.3 |
| Yan’an, China,Lu et al [12] | 9-73 | 12-87 | 259-1055 | 0.2-1.0 | 101-177 | 0.5-0.9 |
| Urumqi, China Ding et al [36] | 20-87 | 12-48 | 273-981 | 0.2-0.9 | 28-110 | 0.2-0.7 |
| Vhangzhi, China, Yang et al [37] | 15-131 | 10-139 | 96-819 | 0.1-1.4 | 17-179 | 0.1-1.1 |
| SW-coastal, India Khandaker et al [38] | 21-54 | 21-65 | 290-440 | 0.3-0.7 | 35-83 | 0.2-0.5 |
| Cuddalore,TN, India, Rajamannan et al [39] | 10-31 | 25-70 | 117-416 | 0.2-0.6 | 24-74 | 0.1-0.5 |
| Una, H.P.,India, Bala et al [40] | 28-236 | BDL-146 | 1060-1583 | 0.4-2.0 | 57-263 | 0.4-1.6 |
| N.E.,Haryana,India, Gupta et al [41] | 18-156 | 23-300 | 32-1705 | 0.2-2.6 | 46 24-324 | 0.2 0.1-0.3 |
| E.Khasi, Megh.India, Lyngkhoi et al [42] | 47 4-93 | 58 14-112 | 312 41-777 | 0.6 0.1-1.1 | 70 12-143 | 0.4 0.1-0.9 |
| India, Kumar et al [43] | 44 | 64 | 456 | 0.6 | 78 | 0.5 |
| India, Sharma et al [44] | 37 24-61 | 99 22-212 | 1536 639-2424 | 1.1 0.5-2.0 | 266 125-468 | 1.7 0.9-3.3 |
| Present study | 39 22-60 | 90 23-198 | 1313 431-2008 | 1.0 0.5-1.9 | 243 117-431 | 1.7 0.8-3.0 |

Italic numbers are the values after re-evaluation using eqns (2), (3) & (4), BDL-below detectable limit

REFERENCES:

- Nambi KSV,  Bapat VN, David M, Sundaram VK, Sunta CM and Soman SD. Natural background radiation and population dose distribution in india. Health physics division bhabha atomic research centre bombay, india. 1986.

- United Nations Scientific Committee on the Effects of Atomic Radiation (UNSCEAR). Sources, effects, and risks of ionizing radiation. United Nations Publications, New York, USA. (1988).

- Arogunjo AM, Farai IP, Fuwape IA.. Dose rate assessment of terrestrial gamma radiation in the delta region of Nigeria. RadiatProt Dosimetry. 108:73‑7 (2004). DOI: 10.1093/rpd/nch010

- ICRP-1999, Protection of the public in situations of prolonged radiation exposure. Publication 82, Ann. ICRP 29(1-2), Elsevier Sciences, B.V. International Commission on Radiological Protection. (1999).

- Zastawny A, Kwasniewicz E, Rabsztyn B. Measurement of the 232Th, 238U and 40K concentration in some samples of ashes from power stations in Poland. Nukleonika. 24: 535 (1979).

- Kant K, Rashmi, sonkawade RG, Sharma GS, Chauhan RP, Chakarvati SK. Seasonal variation of radon, thorn and their progeny levels in dwellings of Haryana and Western Uttar Pradesh. Iran J Radiat Res. 7: 79-84 (2009). http://ijrr.com/article-1-540-en.html

- Sathish LA, Nagaraja K, Ramanna HC, Nagesh V, Sundareshan S. Concentration of radon, thorn and their progeny levels in different types of floorings, walls, rooms and building materials. Iran J Radiat Res. 7: 1-9 (2009).  http://ijrr.com/article-1-523-en.html

- American Cancer Society, Lung Cancer Risk Factors. American Cancer Society (2016). http://www.cancer.org>...>Lung.

- Li C., Wang Ch., Yu J., Fan Y., Liu D., Zhou W., Shi T., Residential radon and histological types of lung cancer: A meta-analysis of case-control studies. Int J Enviro Res Public Health. 17: 1457 (2020). DOI: 10.3390/ijerph17041457

- United Nations Scientific Committee on the Effects of Atomic Radiation (UNSCEAR). Sources and effects of ionizing radiation. United Nations Publications, New York, USA. (2000).

- Papastefanou C, Stoulos S &Manolopoulou M. The radioactivity of building materials. Journal of Radioanalytical and Nuclear Chemistry. 266: 367-372 (2005). doi:10.1007/s10967-005-0918-z

- Lu X, Li N, Yang G & Zhao C. Assessment of natural radioactivity and radiological hazards in building materials used in Yan’an, China. Health Phys. 104(3); 325-331 (2013). DOI: 10.1097/HP.0b013e31827a7ea2

- Manipur population, list of district of Manipur, India, 2011. Census of India.   https://censusindia.gov.in/nada/index.php/catalog/43013, last accessed on 10 Oct. 2024.

- Sharma BA, Singh SN, Singh NS, Singh HN. Measurement of natural radioactivity of building materials used in the southern valley region of Manipur, India. Radiat Prot Environ. 43: 82 -7 (2020). DOI:10.4103/rpe.RPE_12_20

- Suranjit S., Singh O.S., Singh S.N., Sharma B.A., Assessment of radioactivity of different types of houses in Imphal city, Manipur, India. Radiat Prot Environ. 43: 26-30 (2020). DOI: 10.4103/rpe.RPE_42_19

- Singh HS, Devi AR, Sharma BA, Natural radioactivity of building materials used in the Thoubal and Bishnupur districts of Manipur, India. Book chapter 4, Current perspective to Physical Science Research; BP International publisher. 9: 31-46 (2024).

- Roth J, Schweizer P., Guckel C., Basis of Radiation Protection. Pubmed. 126(26):1157-7 1 (1996).

- El-Taher A. Assessment of natural radioactivity levels and radiation hazards for building materials used in Quassim Area, Saudi Arabia. Rom. J. Phys. 57(3-4):726-735 (2012).

- Vanasundari K., Ravisankar R., Durgadevi D., Kavita R., Karthikeyan M., Thillivelvan K., Dhinakaran B. Measurement of Natural Radioactivity in Building Material Used in Chengam of Tiruvannamalai District, Tamilnadu by Gamma-Ray Spectrometry. Indian J Advances in Chemical Sci. 22-27 (2012).

- Ademola A.K., Olaoye M.A., Abodunrin P.O. Radiological safety assessment and determination of heavy metals in soil samples from some waste dumpsites in Lagos and Ogun state, south-western, Nigeria. J Radiat Res Appl Sci. 8:148-153 (2015). https://doi.org/10.1016/j.jrras.2014.12.010

- Sharma BA, Singh NS, Devi PT, Basu H, Saha S, Singhal RK. Assessment of radioactivity in the soil samples from Imphal city, India, and its radiological implication. Radiat Prot Environ. 40: 149-53 (2017). DOI:10.4103/rpe.RPE_28_17

- Singh, S.N., Sharma, B.A., & Devi, T.P. Study of natural radioactivity (226Ra, 232Th, and 40K) in soil samples for the assessment of average effective dose and radiation hazard parameters. Radiat Prot Environ. 40:154-8 (2017). DOI: 10.4103/rpe.RPE_29_17

- Joyshangkar M, Suranjit S, Singh S N, Sharma BA, Singh R T, Measurement of terrestrial gamma radiation dose rate and radioactivity levels in the southern hilly regions of Manipur, India. Radiat Prot Environ. 43:13-20 (2020). DOI: 10.4103/rpe.RPE_40_19

- Singh HS, Singh NP, Singh TB, Sharma BA, Assessment of radioactivity of soil of Thoubal district, Manipur. Eur Chem Bull. 11(12):4921-4925 (2022). DOI: 10.53555/ecb.v11:i12.17737

- Al-Zahrani, J. H., Estimation of natural radioactivity in local and imported polished granite used as building materials in Saudi Arabia, J Radiat Res Appl Sci. Available from: http://dx.doi.org/10.1016/j.jrras.2017.05.001,last accessed on 24 Nov.2023. (2017).

- EC (European commission) Radiation Protection 112- Radiological Protection Principles Concerning the Natural Radioactivity of Building Materials Directorate General Environment. Nuclear Safety and Civil Protection. (1999).

- Rao DD, Effective doses from terrestrial radiation and their comparison with reference levels. Radiat. Prot. Environ. 39: 51-2 (2016). DOI:10.4103/0972-0464.190397

- OECD, Exposure to Radiation from Natural Radioactivity in Building Materials. Report by a Group of Experts of the OECD (Paris: Nuclear Energy Agency). Organization for Economic Co-operation and Development. 1979.

- Trevisi R., Alessandro M. D., Nuccetelli C., Risica S., Radioactivity in Building Materials: a first overview of the European scenario.  International congress of the International Radiation Protection Association (IRPA): Strengthening radiation protection worldwide; Buenos Aires (Argentina); 19-24 Oct (2008).

- Rahman S., Faheem M., Matiullah, Natural radioactivity measurements in Pakistan – an overview. J Radiol Prot. 28: 443-452 (2008). doi: 10.1088/0952-4746/28/4/R01

- Al-Jundi J., Salah W., Bawa’aneh M. S., Afaneh F., Exposure to radiation from the natural radioactivity in Jordanian building materials. Radiat Prot Dosimetry. 118(1): 93-6 (2006). DOI:10.1093/rpd/nci332

- Turhan S., Baykan U. N., Sen K., Measurement of the natural radioactivity in building materials used in Ankara and assessment of external doses. J Radiol Prot. 28(1): 83-91 (2008). DOI: 10.1088/0952-4746/28/1/005

- Cetinkaya H., Manisa K., Isik U., Radioactivity content of building materials used in Kutahya province, Turkey. Radiat Prot Dosimetry. 198(3): 167-174 (2022). DOI: 10.1093/rpd/ncac012

- Garba N. N., Rabi’u N., Aliyu A. S., Kankara U. M., Vasta A. M., Isma’ila A., Bello S., Evaluation of radiological risk associated with local building materials commonly used in Northwestern Nigeria. Heliyon. 9(5): e15791 (2023). DOI: 10.1016/j.heliyon.2023.e15791

- Abbasi A, Calculation of gamma radiation dose rate and radon concentration due to granites used as building materials in Iran. Radiat Prot Dosimetry. 155(3): 335-42 (2013). DOI:10.1093/rpd/nct003

- Ding X., Lu X., Zhao C., Yang G., Li N., Measurement of natural radioactivity in building materials used in Urmqi, China. Radiat Prot Dosimetry. 155(3): 374-9 (2013). DOI: 10.1093/rpd/nct002

- Yang G., Lu X., Zhao C., Li N., Natural radioactivity in building materials used in Changzhi, China. Radiat Prot Dosimetry. 155(4): 512-6 (2013). DOI: 10.1093/rpd/nct018

- Khandaker M. U., Jojo P. J., Kassim H. A., Amin Y. M., Radiometric analysis of construction materials using HPGe gamma-ray spectrometry. Radiat Prot Dosimetry. 152(1-3): 33-7 (2012). https://doi.org/10.1093/rpd/ncs145

- Rajamannan B., Viruthagiri G., Jawahar K. S., Natural radionuclides in ceramic building materials available in Cuddalore district, Tamil Nadu, India. Radiat Prot Dosimetry. 156(4): 531-4 (2013). DOI: 10.1093/rpd/nct092

- Bala P., Mehra R., Ramola R. C., Distribution of natural radioactivity in soil samples and radiological hazards in building material of Una, Himachal Pradesh. Journal of Geochemical Exploration. 142: 11-5 (2014). http://dx.doi.org/10.1016/j.gexplo.2014.02.010

- Gupta M., Chauhan R.P., Eastimating radiation dose from building materials. Iran J Radiat Res. 9(3): 187-194 (2011).

- Lyngkhoi B., Nongkynrih P., Radioactivity in building materials and assessment of risk of human exposure in the east Khasi Hills District, Meghalaya, India. Egyptian Journal of Basic and Applied Sciences. 7(1): 194- 209 (2020).

https://doi.org/10.1080/2314808X.2020.1781747

- Kumar V., Ramachandran T.V., Prasad R., Natural radioactivity of Indian building materials and by- products. Appl Radiat Isot. 51: 93-6 (1999). https://doi.org/10.1016/S0969-8043(98)00154-7.

- Sharma BA & Devi AR., Assessment of natural radioactivity in the RCC building materials used in the valley region of Manipur, India. Rad Prot Dosim. 200(10): 938-944 (2024). DOI: 10.1093/rpd/ncae142